| TEST | UNITS | TEST METHOD | SPECIFICATION | TYPICAL VALUES |
| --- | --- | --- | --- | --- |
| DENSITY AT 15 °C | kg/m3 | ASTM D1298/ ASTM D7042 | REPORT | 852 |
| KINEMATIC VISCOSITY AT 100 °C | mm²/s | ASTM D445/ ASTM D7042 | 2,90 MINIMUM | 3203 |
| KINEMATIC VISCOSITY AT 40 °C | mm²/s | ASTM D445/ ASTM D7042 | 11,00 - 14,50 | 11,89 |
| VISCOSITY INDEX | DIMENSIONLESS | ASTM D2270 | 135 MINIMUM | 141 |
| DYNAMIC BROOKFIELD VISCOSITY AT -40 °C | mPa*s | ASTM D2983 | 3 500 MAXIMUM | 2 000 |
| POUR POINT | °C | ASTM D97 | REPORT | -54 |
| FLASH POINT AT 101,3 kPa, CLEVELAND OPEN CUP | °C | ASTM D92 | 154 MINIMUM | 168 |
| 4-BALL WEAR TEST METHOD (600 rpm /40 kg /93 °C) | mm | ASTM D4172 | 0,47 MAXIMUM | 0,39 |
| FOAMING CHARACTERISTICS (SEQUENCE I) | ml/ml | ASTM D892 | 70/0 MAXIMUM | 20/0 |
| FOAMING CHARACTERISTICS (SEQUENCE II) | ml/ml | ASTM D892 | 50/0 MAXIMUM | 30/0 |
| FOAMING CHARACTERISTICS (SEQUENCE III) | ml/ml | ASTM D892 | 70/0 MAXIMUM | 20/0 |
| MOISTURE BY CRACKLE TEST | NA | CLIENT METHOD (91300029) | NEGATIVE | NEGATIVE |
| - Notes: The active version of the applicable method shall be the version issued and provided by the laboratory. |  |  |  |  |

CUSTOMER’S APPROVAL

| # Elaborated and approved by: | # Research & Development |
| --- | --- |
| # Folio APQP | 04-25-AMO-0003 |
| # Folio VAP | # --- |
| # Part ID | # 20100043 |
| # Date | # 09/10/2026 |
| # Revision | # 01 |
| # Customer’s Name |  |
| # Customer’s Revision Number | # --- |

COMPANY:

NAME:

POSITION:

DATE:

SIGNATURE: