| TEST | UNITS | TEST METHOD | SPECIFICATION | TYPICAL VALUES |
| --- | --- | --- | --- | --- |
| SAYBOLT COLOR | N/A | ASTM D156 | +20 MINIMUM | +30 |
| DENSITY AT 25 °C | g/cm3 | ASTM D1298/ ASTM D7042 | 0,820 - 0,890 | 0,870 |
| KINEMATIC VISCOSITY AT 100 °C | mm²/s | ASTM D445/ ASTM D7042 | 22,50 MINIMUM | 26 |
| KINEMATIC VISCOSITY AT 40 °C | mm²/s | ASTM D445/ ASTM D7042 | 250 - 350 | 309,1 |
| FLASH POINT AT 101,3 kPa, CLEVELAND OPEN CUP | °C | ASTM D92 | 260 MINIMUM | 270 |
| ANILINE POINT, METHOD E | °C | ASTM D611 | 115 MINIMUM | 125 |
| CARBON TYPE COMPOSITION (%CA, %CN, %CP) | --- | ASTM D2140 | --- | --- |
| PERCENTAGE OF AROMATIC RING CARBONS (%CA) | % | ASTM D2140 | 1 MAXIMUM | 0 |
| PERCENTAGE OF NAPHTHENIC RING CARBONS (%CN) | % | ASTM D2140 | REPORT | 29 |
| PERCENTAGE OF PARAFFINIC CHAIN CARBONS (%CP) | % | ASTM D2140 | REPORT | 71 |
| MOISTURE BY CRACKLE TEST | NA | CLIENT METHOD (91300029) | NEGATIVE | NEGATIVE |
| - Notes: The active version of the applicable method shall be the version issued and provided by the laboratory. |  |  |  |  |

CUSTOMER’S APPROVAL

| # Elaborated and approved by: | # Research & Development |
| --- | --- |
| # Folio APQP | - |
| # Folio VAP | # - |
| # Part ID | # 20300163 |
| # Date | # 09/10/2026 |
| # Revision | # 01 |
| # Customer’s Name |  |
| # Customer’s Revision Number |  |

COMPANY:

NAME:

POSITION:

DATE:

SIGNATURE: